| Alloy Code | AlphaSoft120 | Colour | Green yellow | KT | 10K – 18K |
| --- | --- | --- | --- | --- | --- |

| General Information |  |  |  |  |  | Properties |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AlphaSoft120 is a Green yellow alloy. |  |  |  |  |  | Melting Point | 820°C |
|  |  |  |  |  |  | Flow Point | 845 °C |
| Nominal Composition: |  |  |  |  |  | Density | 12,7 g/cm³ |
| AG | CU | ZN | NI | Other |  |  |  |
| 3 | 1 | 2 | 5 | 4 |  |  |  |
| *1=most, 5=least |  |  |  |  |  |  |  |
| Typical Applications: Stamping – Tube - Chain |  |  |  |  |  |  |  |

| Working Characteristics |  |  |  |  |
| --- | --- | --- | --- | --- |
| Casting | Stamping | Tube | Chain | Enameling |
| * | ***** | ***** | ***** | *** |
| ***** Excellent **** Good *** Fair ** Poor * Not Recommended Hardenable by Heat: Yes |  |  |  |  |

| Mechanical Characteristics |  |  |  |  |
| --- | --- | --- | --- | --- |
| Vickers Microhardness After Casting HV 0,5 |  |  |  |  |
| 9K | 10K | 14K | 18K | 22K |
|  | 100 | 117 |  |  |
| Vickers Microhardness After Hardening HV 0,5 |  |  |  |  |
| 9K | 10K | 14K | 18K | 22K |
|  | 108 | 122 |  |  |
| Tensile Strength After Casting N/mm² |  |  |  |  |
| 9K | 10K | 14K | 18K | 22K |
|  | 440 | 523 |  |  |
| Elongation After Casting (A%) |  |  |  |  |
| 9K | 10K | 14K | 18K | 22K |
|  | 30 | 36 |  |  |

| Lost-Wax Casting Process |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Casting Temperature |  |  | Flask Temperature |
| 9 K |  |  |  |  |
| 10 K |  |  |  |  |
| 14 K |  |  |  |  |
| 18 K |  |  |  |  |
| 22 K |  |  |  |  |
| - Choose lower temperatures for centrifugal machines. - As a general acception, using lower temperatures for thick designs and higher temperatures for thin designs would be recommended. |  |  |  |  |
| Quenching |  |  | Heat Treatment |  |
| After casting cooling time for the flasks is 20 minute (for stone casting 60 minute). |  |  | Hardening: 1) Keep at 750 °C for 1 hour then cool immediately. 2) Keep at 350 °C for 3 hours and then cool slowly. |  |

Annealing:

Keep at 650 °C for 30 min. and then

quench in hot water.

Material can be worked to max.%50

reduction, then it must be annealed.

7/24 Call Center: +90-555-813 7272

*** For more information, please request charts from our technical service.

Chart-1	: Investment Process		Chart-2	: Burnout Process

Chart-3	: Melting Process		Chart-4	: Support-sprue systems