| Alloy Code | AlphaSoft253 | Colour | White | KT | 10K-18K |
| --- | --- | --- | --- | --- | --- |

| General Information |  |  |  |  |  | Properties |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AlphaSoft253 is a palladium-free white alloy. |  |  |  |  |  | Melting Point | 830 °C |
|  |  |  |  |  |  | Flow Point | 910 °C |
| Nominal Composition: |  |  |  |  |  | Density | 10,1 g/cm³ |
| AG | CU | ZN | NI | Other |  |  |  |
|  | 1 | 2 | 3 | 4 |  |  |  |
| *1=most, 5=least |  |  |  |  |  |  |  |
| Typical Applications: Stamping – Tube - Chain |  |  |  |  |  |  |  |

| Working Characteristics |  |  |  |  |
| --- | --- | --- | --- | --- |
| Casting | Stamping | Tube | Chain | Enameling |
| ** | ***** | ***** | ***** | **** |
| ***** Excellent **** Good *** Fair ** Poor * Not Recommended Hardenable by Heat: Yes |  |  |  |  |

| Mechanical Characteristics |  |  |  |  |
| --- | --- | --- | --- | --- |
| Vickers Microhardness After Casting HV 0,5 |  |  |  |  |
| 9K | 10K | 14K | 18K | 22K |
|  | 112 | 128 |  |  |
| Vickers Microhardness After Hardening HV 0,5 |  |  |  |  |
| 9K | 10K | 14K | 18K | 22K |
|  | 165 | 205 |  |  |
| Tensile Strength After Casting N/mm² |  |  |  |  |
| 9K | 10K | 14K | 18K | 22K |
|  | 480 | 520 |  |  |
| Elongation After Casting (A) % |  |  |  |  |
| 9K | 10K | 14K | 18K | 22K |
|  | 45 | 40 |  |  |

| Lost-Wax Casting Process |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Casting Temperature |  |  | Flask Temperature |
| 9 K |  |  |  |  |
| 10 K |  |  |  |  |
| 14 K |  |  |  |  |
| 18 K |  |  |  |  |
| 22 K |  |  |  |  |
| - Choose lower temperatures for centrifugal machines. - As a general acception, using lower temperatures for thick designs and higher temperatures for thin designs would be recommended. |  |  |  |  |
| Quenching |  |  | Heat Treatment |  |
| After casting cooling time for the flasks is 20 minute (for stone casting 60 minute). |  |  | Hardening: 1) Keep at 750 °C for 1 hour then cool immediately. 2) Keep at 400 °C for 3 hours and then cool slowly. Annealing: Keep at 700 °C for 30 min. and then cool in air |  |

7/24 Call Center: +90-555-813 7272

*** For more information, please request charts from our technical service.

Chart-1	: Investment Process		Chart-2	: Burnout Process

Chart-3	: Melting Process		Chart-4	: Support-sprue systems