| Alloy Code | AlphaSol818 | Colour | Yellow | KT | 18K |
| --- | --- | --- | --- | --- | --- |

| General Information |  |  |  |  |  |  | Properties |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AlphaSol818 is a yellow alloy |  |  |  |  |  |  | Melting Point |  | 770 °C |  |
|  |  |  |  |  |  |  | Flow Point |  | 810 °C |  |
| Nominal Composition: |  |  |  |  |  |  | Density |  |  |  |
| AG | CU | ZN | NI | Other |  |  |  |  |  |  |
| 1 | 2 | 4 |  | 3 |  |  |  |  |  |  |
| *1=most, 5=least |  |  |  |  |  |  |  |  |  |  |
| Typical Applications: Solder |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  | Heat Treatment |  |  |

Annealing:

Keep at 650 °C for 30 min. and then

quench in hot water.

7/24 Call Center: +90-555-813 7272

*** For more information, please request charts from our technical service.

Chart-1	: Investment Process		Chart-2	: Burnout Process

Chart-3	: Melting Process		Chart-4	: Support-sprue systems